## Slide 1: Defect-induced ferroic states in solid solutions of layered van der Waals materials
Paula Giraldo-Gallo
Universidad de Los Andes
Bogotá, Colombia
5th Workshop on Statistical Physics- April of 2026
Ferromagnetic semiconductor
Ferroelectric
semimetal
Multiferroic semiconductor
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Notes: All at room temperature

## Slide 2
2D - Van der Waals materials
P. Ajayan et al., Physics Today 69, 9, 38 (2016).
S. Manzeli et at., Nat. Rev. 2 (2017) 17033
MX2
Transition metal dichalcogenides
Semiconducting
MoS2, MoSe2 (2H)
WS2, WSe2
Metallic
NbS2, NbSe2 , NbTe2, TaS2, TaSe2, WTe2, MoTe2 (1T’)
Promotes ferroic states which are robust to dimensional confinement!

## Slide 3
Ferroic orders and multiferroicity
Ferroelectricity
Ferroelasticity
Spaldin N. & Fiebig M., Science 309 (2005) 391-392.
Magnetoelectric multiferroics
Electric-field controlled magnetic data storage
Multifunctional devices: single device, multiple tasks.
Magnetically modulated piezoelectrics
Individual ferroic states
Non-volatile data storage
FeRAM (ferro-electric RAM)
MeRAM (Magneto-electric RAM)
Ferromagnetism
Controlled by

## Slide 4
Ferroic orders in TMDs: Ferromagnetism
MoS2 (bulk)
V-doped WSe2 (monolayer)
Appl. Phys. Lett. 101, 123105 (2012).
1T-VSe2 (monolayer)
PRL 110, 247201 (2013)
@RT, proton irr.
J. Am. Chem. Soc. 2015, 137, 2622−2627
Nanoscale 9 (2017) 4898
Nat. Nanotech.
13 (2018) 289
Fe-doped MoS2 (monolayer)
Nat. Comm.
11 (2020) 2034
  Adv. Mater. 34 (2022) 2106551
MoS2 (nanosheets)
WSe2 (nanosheets)

## Slide 5
Ferroic orders in TMDs: Ferromagnetism
Appl. Phys. Lett. 101, 123105 (2012).
PRL 110, 247201 (2013)
@RT, proton irr.
J. Am. Chem. Soc. 2015, 137, 2622−2627
Nanoscale 9 (2017) 4898
Nat. Nanotech.
13 (2018) 289
Nat. Comm.
11 (2020) 2034
  Adv. Mater. 34 (2022) 2106551
MoS2 (bulk)
V-doped WSe2 (monolayer)
1T-VSe2 (monolayer)
Fe-doped MoS2 (monolayer)
MoS2 (nanosheets)
WSe2 (nanosheets)
DEFECTS!

## Slide 6
Ferroic orders in TMDs: Ferromagnetism
Appl. Phys. Lett. 101, 123105 (2012).
PRL 110, 247201 (2013)
@RT, proton irr.
J. Am. Chem. Soc. 2015, 137, 2622−2627
Nanoscale 9 (2017) 4898
Nat. Nanotech.
13 (2018) 289
Nat. Comm.
11 (2020) 2034
  Adv. Mater. 34 (2022) 2106551
MoS2 (bulk)
V-doped WSe2 (monolayer)
1T-VSe2 (monolayer)
Fe-doped MoS2 (monolayer)
MoS2 (nanosheets)
WSe2 (nanosheets)
DEFECTS!
CRYSTALLINE ENVIRONMENT  1T!
DOPANTS

## Slide 7
Ferroic orders in TMDs: Ferroelectricity
1Td-WTe2 (bulk)
Science adv. 5 (2019) eaax5080
SS-PFM
domain orientation
deformation
Khanbareh,, TU Delft (2016).
Piezoelectricity
Notes: Ss-pmf  switching spectroscopy PFM

## Slide 8
Ferroic orders in TMDs: Ferroelectricity
1Td-WTe2 (bulk)
Science adv. 5 (2019) eaax5080
domain orientation
deformation
Khanbareh,, TU Delft (2016).
Piezoelectricity
WSe2 (monolayer)
Nano Energy 52 (2018) 117
Non-centrosymmetric structures
Nature 514 (2014) 470
Notes: Ss-pmf  switching spectroscopy PFM

## Slide 9
General Strategy
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
Solid solution
(ferro)magnetic semiconductor
Ferroelectric
semimetal
Khomskii, D. Physics, 2 (2020) 20.
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Generate/strengten FM in bulk material
  survives to nanostructuration
Move FE state into semiconducting regime  memories!
No need for nanostructuring to the monolayer limit
Create multiferroics  Multifunctional platform
DEFECTS!
1T CRYSTALLINE ENVIRONMENT
DOPANTS

## Slide 10
Single crystal growth
1 mm
Solid solution single crystals
Synthesis by chemical vapor transport
Chalcogen vacancies (δ>0)
XRF
Solid solution
(ferro)magnetic semiconductor
Ferroelectric
semimetal
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Chalcogen interstitial (δ<0)
Lowest formation energy

## Slide 11
Single crystal growth
(ferro)magnetic semiconductor
Ferroelectric
semimetal
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Solid solution
Ramón Támara, PGG, et al., In preparation (2026)

## Slide 12
WSe2WTe2 Phase Diagram
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)

## Slide 13
WSe2WTe2 Phase Diagram
x
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)

## Slide 14
WSe2WTe2 Phase Diagram
δ
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)

## Slide 15
WSe2WTe2 Phase Diagram
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
δ<0
(Se,Te) interstitials
δ>0
(Se,Te) vacancies

## Slide 16
WSe2WTe2 Phase Diagram
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
vacancies
Interstitials

## Slide 17
WSe2WTe2 Phase Diagram
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
vacancies
Interstitials

## Slide 18
WSe2WTe2 : Magnetism
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Coercive Field
Vacancies strenghten Ferromagnetism

## Slide 19
Ferromagnetism in W(Se1-xTex)2(1-δ): Possible mechanism
DFT calculations in systems which closely resemble (x,δ) values for experimental samples
Realization 1:
x=10%, δ=39%
Realization 2:
Ferromagnetic
Non-magnetic
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
Notes: Simulations in 4x4x1 supercell (96 atoms)
Magnetic momento of order 0.1 uB/unit cell

## Slide 20
WSe2WTe2 : Ferroelectricity
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
WSe2 (monolayer)
Nano Energy 52 (2018) 117
Para/piezoelectric

## Slide 21
WSe2WTe2 : Ferroelectricity
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Para/piezoelectric
x=7.6%, δ=38%
x=15%, δ=21%

## Slide 22
Ferroelectricity in W(Se1-xTex)2(1-δ): Possible mechanisms
Mechanisms contemplated in literature:
Non-centrosymetric crystal structure X
Sliding ferroelectricity ?
Vacancy induced ?
Our DFT simulations:
Unit cell electric polarization through Berry-phase
Hirshfeld charge analisis for local dipole formation
Pristine 2H-WSe2 case: non-polar (c-axis)
-2q
+q
+q
Se
W
Se
Effect of vacancies: breaks local centrosymmetry  c-electric dipole
Electric dipole moment for Te-W dipoles: 20 times bigger!
-2q
+q
Se
W
Se
-2q
+q
Se
W
Se
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Notes: D33-PPLN=19 pm/V

## Slide 23
WSe2WTe2 : Ferroic Phase diagram
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)

## Slide 24
Ferroic properties
in other solid solutions
(ferro)magnetic semiconductor
Ferroelectric
semimetal
Ramón Támara, PGG, et al., In preparation (2026)
Ferromagnetic
Ferroelectric
BULK

## Slide 25
2um
electrode (+)
electrode (-)
Ferroic properties
in other solid solutions
(ferro)magnetic semiconductor
Ferroelectric
semimetal
Ramón Támara, PGG, et al., In preparation (2026)
Ferromagnetic
Ferroelectric
BULK
NANOSTRUCTURES
Monolayer!
Valentina Posada, PGG, et al., In preparation (2026)

## Slide 26: Acknowledgements
Prof. Camilo Espejo
U. Norte, COL – (DFT - calculations)
Prof. William López
Prof. Jose A. Galvis
U. Rosario, U. Central, COL (Microscopy)
Prof. Alejandro Castañeda
Prof. Oscar Herrera
Harold Rojas (PhD)
Ramón Támara (master)
Valentina Posada (und.)
Edwin Ramos
Camila Riveros
J. D. Santacruz
Brayan Walteros
Lina Rodríguez
David Santa
Juan A. Puyo
Noah Lodoño

## Slide 27: Defect-induced ferroic states in solid solutions of layered van der Waals materials
Paula Giraldo-Gallo
Universidad de Los Andes
Bogotá, Colombia
5th Workshop on Statistical Physics- April of 2026
Ferromagnetic semiconductor
Ferroelectric
semimetal
Multiferroic semiconductor
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
Notes: All at room temperature

## Slide 28
Transition metal dichalcogenides - TMDs
MX2
Between planes: Chalcogen-chalcogen van-der Waals interaction (weak)
In plane: T. Metal-chalcogen covalent bonds (strong)
Low dimensional character
Exfoliation down to monolayers
Quasi-2D compounds
S. Manzeli et at., Nat. Rev. 2 (2017) 17033
Semiconducting
MoS2, MoSe2 (2H)
WS2, WSe2
Metallic
NbS2, NbSe2 , NbTe2, TaS2, TaSe2, WTe2, MoTe2 (1T’)
Applications:
Optoelectronics, spintronics, thermoelectrics, electronic devices
Applications:
Energy, spintronics, switches, quantum computing
Phenomena:
Indirect to direct gap in the monolayer limit
Plenomena:
Charge density wave, superconductivity, topological

## Slide 29
Transition metal dichalcogenides - TMDs
MX2
Quasi-2D compounds
C.M.O. Bastos et al., PRM 3 (2019) 044002;
Structural Polytypes

## Slide 30
Ferroic orders and multiferroicity
Ferroelectricity
Ferromagnetism
Ferroelasticity
Requires partially filled d/f orbitals
Spaldin N. & Fiebig M., Science 309 (2005) 391-392.
Typically show empty d orbitals
Typically insulators
Typically metals
Seem incompatible  Scarce in nature
Magnetoelectric multiferroics
Electric-field controlled magnetic data storage
Multifunctional devices: single device, multiple tasks.
Magnetically modulated piezoelectrics
Examples (3D crystal structures):
Boracites: Ni3B7O13I
Perovskites: Pb2(CoW)O6, BiFeO3, BiMnO3, TbMnO3, others.
LuFe2O4

## Slide 31
2D ferroics/multiferroics
Miniaturization of devices
3D ferroics/multiferroics  depolarization at nanoscale
2D ferroics/multiferroics
intrinsic 2D crystal structure: bulk & nanolayer
more robust to quantum confinement effects
Less susceptible to interfacial defects/chemical discontinuities when integrated into semiconductor industry devices
C. Wang et al., Nat. Materials 22 (2023) 542.
Fundamental understanding of long-range order in low-dimensional systems
G. Cardenas-Chirivi, PGG et al. Room temperature multiferroicity in a transition metal dichalcogenide, npj 2D Mat. and Appl. 7 (2023) 54
2D-Multiferroics

## Slide 32
Ferroic orders in TMDs: Ferromagnetism
J. Am. Chem. Soc. 2015, 137, 2622−2627
Nat. Nanotech.
13 (2018) 289
Nat. Comm.
11 (2020) 2034
MoS2 (bulk)
V-doped WSe2 (monolayer)
1T-VSe2 (monolayer)
Fe-doped MoS2 (monolayer)
MoS2 (nanosheets)
WSe2 (nanosheets)
PRL 110, 247201 (2013)
Nanoscale 9 (2017) 4898
@RT, proton irr.
Grain boundary zig-zag edges
Appl. Phys. Lett. 101, 123105 (2012).
  Adv. Mater. 34 (2022) 2106551
M-dangling bonds
Notes: Sig-zag Edges and terminations  different spin densities depending on termination, moments localized around Se-p orbitals
Proton irradiation  spin density localized around Mo atoms next to MoS2 vacancies
1T incorporation: S vacancies trigger transformation from trigonal prismatic 2H to octahedral 1T phase locally, introducing Mo 4d states within the gap. Ferro through Exchange between vacancy and Mo 4d states.

## Slide 33
Ferroic orders in TMDs: Ferroelectricity
1Td-WTe2 (bulk)
Science adv. 5 (2019) eaax5080
Khanbareh,, TU Delft (2016).
1Td-WTe2 (bi-trilayer)
Piezoelectricity
Nat. comm. 10 (2019) 1775
Nature 560 (2018) 336
WSe2 (monolayer)
MoS2 (monolayer)
Nature 514 (2014) 470
Nano Energy 52 (2018) 117
1T-MoTe2 (monolayer)
Notes: Ss-pmf  switching spectroscopy PFM

## Slide 34
1T-MoTe2 (monolayer)
Nat. comm. 10 (2019) 1775
Nature 514 (2014) 470
Nano Energy 52 (2018) 117
Ferroic orders in TMDs: Ferroelectricity
1Td-WTe2 (bulk)
Khanbareh,, TU Delft (2016).
1Td-WTe2 (bi-trilayer)
Piezoelectricity
WSe2 (monolayer)
MoS2 (monolayer)
Nature 560 (2018) 336
Science adv. 5 (2019) eaax5080
Broken centrosymmetry in 2H - odd # of layers
Light: Science & Appl. (2016) 5, e16131
Notes: Ss-pmf  switching spectroscopy PFM

## Slide 35
Multiferroicity in TMDs:
strategy imported from 3D
Spaldin N. & Fiebig M., Science 309 (2005) 391.
Ferroelectric  PbZr1–xTixO3 (PZT)
Ferromagnet Tb1–xDyxFe2 (Terfenol-D)
Composites, heterostructures
Solid solution
Single crystals
Fiebig M., J. Phys. D: Appl. Phys. 38 (2005) R123.
(ferro)magnetic semiconductor
Ferroelectric
semimetal
In the TMDs’ world

## Slide 36
Single crystal growth
1 mm
Te-doped single crystals
Synthesis by chemical vapor transport
Chalcogen vacancies
(Also molten flux technique, in Te or Sb fluxes)
XRF
G. Cardenas-Chirivi et al. Room temperature multiferroicity in a transition metal dichalcogenide, npj 2D Mat. and Appl. 7 (2023) 54

## Slide 37
WSe2WTe2 Phase Diagram
x < 30%  2H
x > 80%  1Td
30% < x < 80%
2H + 1Td
Crystal structure
G. Cardenas-Chirivi, PGG et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas, PGG et al., arXiv:2603.08515 (2026)
vacancies
Interstitials

## Slide 38
structural properties

## Slide 39
WSe2WTe2 structural properties
Te-doped single crystals
Chalcogen vacancies
XRF
X-ray diffraction
2H crystal structure for all dopings studied (x<15%)
(XRD – powder and single crystal)
Increase in lattice parameters  ()
No signatures of 1Td structure
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)

## Slide 40
WSe2WTe2 structural properties
Te-doped single crystals
Chalcogen vacancies
XRF
2H crystal structure for all dopings studied (x<15%)
(XRD – powder and single crystal)
Increase in lattice parameters  ()
Raman spectroscopy
WSe2
1Td (, )
2H
Te-doping
No signatures of 1Td structure
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)
Notes: Agregar líneas de raman para fase WTe2

## Slide 41
Ferromagnetism in W(Se1-xTex)2(1-δ): Possible mechanism
DFT calculations in systems which closely resemble (x,δ) values for experimental samples
Realization 1:
x=10%, δ=39%
Ferromagnetic
At Fermi level: net magnetization more spin-up than spin-down
At Fermi level: major contribution from W d-orbitals
DOS for spin-up and spin-down electrons
Projected DOS onto atomic orbitals
Suggests that magnetism comes from
transition metal ion
d-electrons
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)
Notes: Simulations in 4x4x1 supercell (96 atoms)

## Slide 42
Magnetic properties of W(Se1-xTex)2(1-δ)
Ferromagnetic
Diamagnetic
VSM - magnetization measurements
@ Room temperature
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)

## Slide 43
Magnetic properties of W(Se1-xTex)2(1-δ)
Ferromagnetic
Diamagnetic
VSM - magnetization measurements
@ Room temperature
2 days
15 days
Diamagnetic component is strongly dependent on oxidation/aging
Ferromagnetic component is more robust (Hc)
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)

## Slide 44
Magnetic properties of W(Se1-xTex)2(1-δ)
Ferromagnetic component
@ Room temperature
Chalcogen vacancies seem to drive ferromagnetism
Te doping promotes formation of vacancies
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)
Notes: Te promotes vacancies: Lower electronegativity difference for Te-M bond formation  weaker bond

## Slide 45
Magnetic properties of W(Se1-xTex)2(1-δ)
Ferromagnetic component: variation of Hc and Ms with storage time
G. Cardenas-Chirivi et al. Room temperature multiferroicity in a transition metal dichalcogenide, arXiv:2212.02490 (2023).
Notes: Masa de las muestras?

## Slide 46
Ferroelectricity in W(Se1-xTex)2(1-δ)
SS-PFM – switching spectroscopy piezoforce microscopy measurements
@ Room temperature
x=1.4%, δ=9%
x=7.6%, δ=38%
x=15%, δ=21%
Enhanced ferroelectricity
Increasing Te concentration (x)
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)
Notes: Ti covered silicon tips for PFM

## Slide 47
Ferroelectricity in W(Se1-xTex)2(1-δ): Piezoelectric coefficient
DART - PFM – Dual AC tracking resonance piezoforce microscopy measurements, @ Room temperature
x=7.6%, δ=38%
x=15%, δ=21%
x=1.4%, δ=9%
PPLN
Highest reported piezoelectric coefficient value for TMDs
Piezoelectricity is strongest for the highest Te-doped sample
G. Cardenas-Chirivi et al., npj 2D Mat. and Appl. 7 (2023) 54
H. Rojas-Paez, PGG, et al., In preparation (2024)
Notes: D33-PPLN=19 pm/V

## Slide 48
Ferroelectricity in W(Se1-xTex)2(1-δ)
SS-PFM – switching spectroscopy piezoforce microscopy measurements
@ Room temperature
G. Cardenas-Chirivi et al. Room temperature multiferroicity in a transition metal dichalcogenide, arXiv:2212.02490 (2023).

## Slide 49
Ferroelectricity in W(Se1-xTex)2(1-δ)
SS-PFM – switching spectroscopy piezoforce microscopy measurements
@ Room temperature
G. Cardenas-Chirivi et al. Room temperature multiferroicity in a transition metal dichalcogenide, arXiv:2212.02490 (2023).

## Slide 50
Ferroelectricity in W(Se1-xTex)2(1-δ): Possible mechanisms
G. Cardenas-Chirivi et al. Room temperature multiferroicity in a transition metal dichalcogenide, arXiv:2212.02490 (2023).
Mechanisms contemplated in literature:
Non-centrosymetric crystal structure
Sliding ferroelectricity
Vacancy induced ?
Our DFT simulations:
Unit cell electric polarization through Berry-phase
Hirshfeld charge analisis for local dipole formation
Pristine 2H-WSe2 case: non-polar (c-axis)
-2q
+q
+q
Se
W
Se
Effect of vacancies: breaks local centrosymmetry  c-electric dipole
Electric dipole moment for Te-W dipoles: 20 times bigger!
-2q
+q
Se
W
Se
-2q
+q
Se
W
Se
Possible dipole switching mechanisms
Intralayer
Interlayer
Notes: D33-PPLN=19 pm/V